Low-Temperature Phase Transition and Crystal Structures of two bicyclic organic molecules

L. Palin1 A. N. Fitch1, 2  M. Brunelli1  J. Wright1  A. J. Mora3, 1

1European Synchrotron Radiation Facility, B.P. 220, F38043 Grenoble Cedex, France 2Department of Chemistry, Keele University, Staffordshire, ST5 5BG, United Kingdom 3Departamento de Quimica, Facultad de Ciencias, Universidad de Los Andes, Merida, Venezuela

The crystal structures of two small organic molecules 7-oxabicyclo[2.2.1]heptane (C6H10O) and norcamphor (C7H10O) have been investigated using synchrotron X-ray powder diffraction at BM16 at the ESRF.  The temperature dependence of the 7-oxabicyclo[2.2.1]heptane and norcamphor  diffraction pattern reveals different solid-state phase transitions. For the 7-oxabicyclo[2.2.1]heptane phase I is between 251 K and 234 K, phase II 234 K-192 K, phase III 191 K-185 K, phase IV below 182 K. For the norcamphor we observed phases between 288 K and 165 K, 164 K-154 K, and below 146 K. The crystal structures in the low-temperature phases of the 7-oxabicyclo[2.2.1]heptane have been studied at 50 K and 185 K. At 50 K the compound is found to be monoclinic, space group P21/a, with a = 24.041 Å, b = 10.259 Å, c = 13.637 Å, β = 102.52° and Z = 24.   The crystal structures in the low-temperature phases of the Norcamphor have been studied at 35 K and 185K. At 35K the compound is found to be monoclinic, space group C21/c, with a = 18.443Å, b = 12.285 Å, c = 13.685 Å, β= 90.96° and Z = 16.