TOPOLOGICAL ANALYSIS OF DEFECTS IN GaN EPITAXIAL FILMS

T-S Huang, R C Pond, P Chalker, Department of Engineering (Materials), University of Liverpool, UK, and G Dimitrakopulos, Department of Physics, Aristotle University, Thessaloniki, Greece.

High quality thin films of GaN are required for microelectronic and optoelectronic devices. In current methods for the epitaxial growth of these films, such as metal-organic chemical vapour deposition and molecular beam epitaxy, substrates of alumina, silicon carbide or silicon substrates are used. Because the lattice parameters and/or spacegroups of these materials are different from the overlying GaN films, the formation of interfacial and bulk defects is promoted. The topological properties of such defects can be predicted  a priori using symmetry theory; their diversity and character depend on the extent of symmetry-breaking accompanying the formation of a bicrystal. Also, when experimental observations of defects have been obtained by techniques such as transmission electron microscopy, circuit-mapping methods can be used a posteriori to characterise linear and planar defects. These crystallographic tools will be illustrated by reference to predicted and experimentally observed defects in epitaxial GaN films.